SECTION 09963 - ELASTOMERIC COATINGS

- GENERAL

      - SUMMARY

        - This Section includes surface preparation and application of textured acrylic and elastomeric coatings to exterior surfaces.

      - PERFORMANCE REQUIREMENTS

        - Provide textured acrylic and elastomeric coatings that are based on 100% acrylic polymers, provide outstanding elongation and flexibility at low temperatures and after exposure to the weather, resistance to mildew growth, rain stain and dirt pickup, and that are highly chalk-resistant.

      - SUBMITTALS

        - Product Data:  For each coating system specified.

        - Samples:  For each color and material to be applied, with texture to simulate actual conditions, on representative Samples of actual substrate(s).

          - Provide stepped Samples, defining each separate coat, including block fillers and primers.  Use representative colors when preparing Samples for review.

          - Provide a list of materials and applications for each coat of each Sample. Label each Sample for location and application.

      - QUALITY ASSURANCE

        - Applicator Qualifications:  A firm or individual experienced in applying coating systems similar in material and extent to those indicated for this Project, whose work has resulted in applications with a record of successful in-service performance.

        - Source Limitations:  Verify crack fillers, block fillers, primers, and other undercoat materials are compatible with coating system. Use products from same manufacturer as finish coats when available.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver materials to Project site in manufacturer's original, unopened packages and containers bearing manufacturer's name and label.

        - Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 40 deg F (4.4 deg C).  Maintain containers used in storage of coatings in a clean condition, free of foreign materials and residue. Do not store longer than 2 years before final use.

          - Protect coating materials from freezing.  Keep materials dry and off of the ground. Keep storage area neat and orderly. Remove waste daily. Take necessary measures to ensure that workers and work areas are protected from health hazards resulting from handling, mixing, and applying the coating.

      - PROJECT CONDITIONS

        - Apply coatings only when temperature of surfaces to be coated and surrounding air temperatures are between 50 and 90 deg F (10 and 32 deg C).

        - Do not apply coatings in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; or at temperatures less than 5 deg F (3 deg C) above the dew point. Allow wet or damp surfaces to dry thoroughly and attain temperature and conditions specified before starting or continuing coating operation.

      - WARRANTY

        - One (1) year Limited Warranty for replacement of defective materials.

- PRODUCTS

      - MANUFACTURERS

        - Magna Wall® Acrylic and Elastomeric Coatings (Textured).

- Magna Wall

- 5014 Callaghan Road

- San Antonio, TX 78228

- Phone: 210.680.3441

- www.magnawall.com

        - Other manufacturer’s product. Any alternative product must meet all specifications as outlined and be approved by the Architect or Designer prior to bidding.

        - Colors and Textures:  As selected by Architect or Designer from manufacturer's full range. Magna Wall® Textured Coatings are offered in three different textures: sand finish, medium finish, and rough finish.

      - ELASTOMERIC FINISH-COAT MATERIALS

        - Textured Acrylic and Elastomeric Finish:  Based upon 100% acrylic polymers.

        - Cautions and Limitations

          - Dark colors may fade.

          - Not for use on interior walls.

          - Not intended to be used as a waterproof coating or for waterproofing below grade.

          - Not for use on submerged surfaces.

          - In-service temperature limit is 200°F.

          - Coatings must not be used on exposed exterior horizontal surfaces. Minimum slope is 27° and maximum width is 12”.

          - Not for use with EIFS.

          - MSDS should be viewed in order to understand all warnings.

- EXECUTION

      - SURFACE PREPARATION

        - General:

          - Remove hardware and accessories, plates, machined surfaces, light fixtures, and similar items already installed that are not to be coated. If removal is impractical or impossible, provide surface-applied protection before surface preparation and coating. After completing coating operations, reinstall items removed, using workers skilled in trades involved.

          - Ensure the area to be coated is in sound condition. A pull-off test may be necessary to ensure the area to be covered is bonded securely to the substrate.

          - All damaged areas, such as loose coatings, cracks, punctures, etc., must be repaired prior to the application of coatings, fillers, or primers.

        - Previously Coated Surfaces:

          - All previously-coated surfaces must be pressure-cleaned to remove all dirt, dust, chalk, mildew, algae, foreign materials, etc.

          - A cementitious primer/basecoat must be applied over entire substrate.

          - If cracking is present, a fiberglass mesh should be embedded into the primer/basecoat for added strength.

        - New Masonry/Poured Concrete Walls:

          - Remove all dirt, oil, grease, mortar, and other compounds that may inhibit a strong bond.

          - A cementitious primer/basecoat may be needed to skim substrate.

          - Concrete or mortar must be thoroughly cured for a period of at least 30 days at 75°F or a QuickCure primer may be used.

        - Stucco Surfaces:

          - Remove all dirt, oil, grease, mortar, and other compounds that may inhibit a strong bond.

          - Stucco surfaces should be cured for 30 days at 75°F or a QuickCure primer may be used, or the pH of the stucco must be 9.0 or lower.

      - MIXING PROCEDURE

        - Mix Magna Wall® Textured Coatings with a 1/2” drill and paddle until workable consistency is attained. Mix can be diluted by adding up to 16 oz. clean potable water.

      - APPLICATION

        - General:  Apply coatings according to manufacturer's written instructions.  Use applicators and techniques best suited for substrate and type of material being applied.

          - Do not apply coatings over conditions detrimental to formation of a durable bond, such as dirt, rust, scale, grease, moisture, and scuffed surfaces.

        - Labels:  Do not apply over UL, FMG, or other code-required labels or equipment name, identification, performance rating, or nomenclature plates.

        - Application Procedures:  Magna Wall® Textured Coatings can be applied with a stainless steel trowel or spray equipment. Use plastic float to achieve desired texture.

        - Drying: Will dry to touch in 3 to 4 hours at 70°F. Protect from rainfall for 24 hours at 70°F. More drying time required when temperature is cooler and/or when relative humidity is higher. Keep product from freezing for 48 hours after application.

        - Completed Work:  Match approved samples for color, texture, and coverage.  Remove, refinish, or recoat work not complying with specified requirements.

      - CLEANING

        - Cleanup:  At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

          - Use soapy water immediately, while coatings are still wet.

          - After completing coating work, clean glass and spattered surfaces.  Remove spattered coatings by washing, scraping, or other methods, being careful not to scratch or damage adjacent finished surfaces.

      - PROTECTION

        - Protect work of other trades whether being coated or not. Correct damage by cleaning, repairing, replacing, and recoating as approved by Architect.  Leave in an undamaged condition.

        - Remove temporary protective wrappings provided by others to protect their work after completing coating operations.

          - After construction activities of other trades are complete, touch up and restore damaged or defaced coated surfaces.

END OF SECTION 09963